BLACK LIQUOR RECOVERY BOILER

ADVISORY COMMITTEE

### MINUTES OF MEETING

### October 7, 2026

OBJECTIVE

BLRBAC’s objective is to promote improved safety of chemical recovery boilers and their auxiliaries through the interchange of technical knowledge, experience, and data on past and any future recovery boiler incidents.	Bylaws - 2.1

OFFICERS

Chairman:     Gregory Burns

Mt Pleasant, SC			                Cell: 843-991-7192

Domtar                                                              gregory.burns@domtar.com

Vice-Chair:    David Tjaarda

Smurfit Westrock                                                         Cell: 503-728-2550

Charleston, TN                                                           dave.tjaarda@smurfitwestrock.com

Secretary:      Daniel Franco

Recovery Specialist                                                Cell: +573113001079

Cali, Colombia                                                        danielf721@gmail.com

Treasurer:      Brad Osbourne

Electron Machine                                                Cell: 352-267-0118

Umatilla, FL                                                      brad@electronmachine.com

REGULAR MEMBERSHIP

Organizations operating, manufacturing, or insuring chemical recovery boilers are eligible.

ASSOCIATE MEMBERSHIP

Organizations having a direct interest or role in the safety of chemical recovery boilers are eligible.

CORRESPONDING MEMBERSHIP

Companies residing outside of the United States which finds it impractical to attend meetings on a regular basis because of distance and expenses, but desires to be involved and informed of BLRBAC activities.

Bylaws - 3.1

BLRBAC INTERNET ADDRESS: ---- www.blrbac.net

IRS Employer ID/Tax ID (IRS E.I.N.T./T.I.N.) ----

EXECUTIVE COMMITTEE

Gregory Burns                                                                                     Jimmy Onstead

BLRBAC Chairman                                                                              Insurance Representative

Domtar                                                                                                 FM Global

Mt Pleasant, SC                                                                                   Frisco, TX

Cell: 843-991-7192                                                                      Tel:  972-731-1656

gregory.burns@domtar.com                                                      Cell: 903-744-2734

jimmy.onstead@fmglobal.com

David Tjaarda                                                                                    Evangelos Townsend (Ev)

BLRBAC Vice Chairman                                                                   Manufacturing Representative

Smurfit Westrock                                                                              Babcock & Wilcox

Charleston, TN                                                                                  Melissa, TX

Cell: 503-728-2550                                                                           Office: (281) 405-6825

dave.tjaarda@smurfitwestrock.com                                              Mobile: (469) 815-8395

emtownsend@babcock.com

Daniel Franco                                                                                   Scott Moyer

BLRBAC Secretary                                                                           Operator Representative

Recovery Specialist                                                                 Smurfit Westrock

Cali, Colombia                                                                        Jacksonville, FL

Cell: +573113001079                                                             Mobile: 904.437.7149

danielf721@gmail.com                                                      scott.moyer@smurfitwestrock.com

Brad Osborne

BLRBAC Treasurer

Electron Machine

Umatilla, FL

Cell: 352-267-0118

brad@electronmachine.com

FUTURE BLRBAC MEETINGS

| Fall | April | 5,6,7 | 2027 |
| --- | --- | --- | --- |
| Fall | October | 4,5,6 | 2027 |

"Bring Operator(s).  Give them a chance to hear firsthand!"

Past Chairman Frank Navojosky

###### *****************************

* NOTE:  For varying reasons, the previously published meeting dates have been changed at the discretion of the Executive Committee.

###### BLRBAC has established its own website at:  www.blrbac.net

At this website you will find a copy of past Meeting Minutes and the next Meeting Notice.  Therefore, each Representative and Associate Representative is asked to inform their people of this WEB site.  This is where they can obtain the following BLRBAC documents:

BLRBAC MEETING NOTICE

COVER LETTER			General Information

REGISTRATION FORM 	Will be available on the website with a link to register and pay on line.

HILTON Airport	Blocked room dates, pricing, address, hotel phone numbers

SCHEDULE				 List of subcommittee activities on Monday and Tuesday

AGENDA	 Reports given to Joint BLRBAC Meeting on Wednesday

OPERATING PROBLEMS	Mail/e-mail completed questionnaires to David Tjaarda

QUESTIONNAIRE	The Vice Chairman will see that your concerns are brought up and discussed during the Operating Problems session at the next meeting.

These are available at the BLRBAC INTERNET ADDRESS: www.blrbac.net

BLRBAC Guidelines & Recommended Practices

LEGAL NOTICE

Recommended Good Practice For Design, Operation, and Testing of the Emergency Shutdown System for Black Liquor Recovery Boilers

(Dated: October 2024)

Safe Firing of Black Liquor in Black Liquor Recovery Boilers

(Dated: October 2023)

Materials & Welding Guidelines

(Dated: April 2025)

Safe Firing of Auxiliary Fuel in Black Liquor Recovery Boilers

(Dated: February 2012)

Fire Protection in Direct Contact Evaporators and Associated Equipment

(Dated: February 2024)

Personnel Safety & Training

(Dated: April 2018)

Application of Rotork Actuators on Black Liquor Recovery Boilers

(Dated: April 2025)

Boiler Water Management Guidelines for Black Liquor Recovery Boiler

(Dated: June 2025)

Instrumentation Checklist and Classification Guide for Instruments and Control Systems Used in the Operation of Black 9Liquor Recovery Boilers (Dated: April 2014)

Thermal Oxidation of Waste Streams in Black Liquor Recovery Boilers

(Dated: June 2021)

If you have any questions, contact:

Secretary:	Daniel Franco		Tel:  +576023258865

Recovery Specialist Retired	Cell: +573113001079

Cali, Colombia                                                         danielf721@gmail.com

BLRBAC SUBCOMMITTEES

| AUXILIARY FUEL Adam Marickovich– Chairman‡ Asset Safety Engineer 850.860.1916 Adam.Marickovich1@gapac.com | BLACK LIQUOR, SAFE FIRING OF Sarah Henke – Chair Valmet North Carolina Tel: 919-454-3441 Sarah.henke@valmet.com |
| --- | --- |
| EMERGENCY SHUTDOWN PROCEDURES Frank Navojosky, Chairman BSI Loveland, OH Cell: (513) 334-9999 fcnavojo@gmail.com | FIRE PROTECTION IN DIRECT CONTACT EVAPORATORS Stephen Cox - Chairman International Paper Maumelle, AR Tel: 409-779-7104 stephen.cox@ipaper.com |
| INSTRUMENTATION John Browning, Chairman Georgia Pacific Atlanta, GA Tel: 251-593-6096 john.browning@GAPAC.com | MATERIALS & WELDING Laura Nicol–Chairperson Babcock & Wilcox 1200 E Market St, Ste 650 Akron, OH 44305 Cell: 330-361-0217 lsnicol@babcock.com |
| PERSONNEL SAFETY Steve Morrison, Chairman Georgia Pacific Corp. Steve.morrison@gapac.com TEAMs – (423) 516-6071 Cell – (423) 480-0119 | PUBLICITY & NEWS RELEASE Nick Quigley - Chairman FM Johnston, RI Cell: +1 401-480-7127 nicholas.quigley@fm.com |
| WASTE STREAMS Paul Seefeld, Chairman A.H. Lundberg Associates, Inc. Jacksonville, FL Tel: 904-614-6492 paul.seefeld@lundberg-us.com | WATER TREATMENT Tom Przybylski, Chairman Power Specialists Associates Somers, CT ### Tel: 860-763-3241 tom.@psaengineering.com |

AUXILIARY FUEL SUBCOMMITTEE

Adam Marickovich– Chairman‡

Asset Safety Engineer

850.860.1916

Adam.Marickovich1@gapac.com

| DeBeer, Tom LCK Consultants, LLC Cell:(404) 218-8613 tdebeer2024@gmail.com | John Lewis‡ General Electric Vernova 200 Great Pond Drive G3W4 Windsor, CT 06095 Tel:(860) 285-2918 john.c.lewis@ge.com | Derrick Gossen‡* FM 301 Freedom Ct. Mishicot, WI 54228 Cell: (920) 619-1750 derrick.gossen@fmglobal.com |
| --- | --- | --- |
| Greg Imig‡ Andritz 5405 Windward Pkwy, Suite 100W Alpharetta, GA 30004 Tel: (770) 640-2633 Cell: (404) 545-9076 greg.imig@andritz.com | Brett GuShue Babcock & Wilcox FPS Inc GshueB@fossil.ca |  |

| ‡ = | Denotes attendance at last meeting, October 7, 2026 |
| --- | --- |
| * = | Denotes a new/replacing member |

EMERGENCY SHUTDOWN PROCEDURES SUBCOMMITTEE

Frank Navojosky– Chairman‡

Boiler Services & Inspection, LLC

BSI

Cell: (513) 334-9999

fcnavojo@gmail.com

| Dean Clay, Secretary‡ Boiler Services & Inspection, LLC BSI Cell: (513) 497-9070 dclayesp@gmail.com | Scott Crysel‡ FM One Cowboys Way, Suite 600 Frisco, TX 75034 Tel: (972) 731-1658 Fax: (972) 731-1820 scott.crysel@fm.com | James Franks‡ AXA XL Risk Consulting 855 Dogwood Road Somerville, TN 38068 Tel: (901) 465-0771 Fax: (888) 964-7348 james.franks@axaxl.com |
| --- | --- | --- |
| Mike Bruce Sylvamo 104 Putnam Center Rd Putnam Station, NY Cell: 518-586-6954 mike.bruce@sylvamo.com | Angelo Porchetta WCBLRBAC Chairman Domtar, Howe Sound Cell: 604-414-8677 angelo.porchetta@domtar.com Alternate: Jason Shaw, GE Vernova‡ Jason.shaw@gevernova.com Cell: 587-337-0543 | David Frazier‡ International Paper Cell: 706-305-75321 david.frazier@ipaper.com |
| Gregory Burns‡ Domtar Cell: (843) 991-7192 Office: 803-802-8077 Fort Mill, SC gregory.burns@domtar.com | Scott Moyer, Vice Chairman ESP‡ Smurfit Westrock Cell: 904-437-7149 scott.moyer@smurfitwestrock.com | Greg Zavadoski‡ Georgia Pacific Cell: 715.432.2470 greg.zavadoski@gapac.com Alternate: Robert Orender, GP robert.orender@gapac.com 470-230-2000 |
| Samuel Miller‡ Andritz Pulp & Paper 5405 Windward Parkway, Suite 100W Alpharetta, GA 30004 Cell: 678-533-9431 samuel.miller@andritz.com | Dan Cudmore‡ GE Vernova 1420 Blair Towers Place Suite 500 Ottawa, ON K1J 9L8 Tel: (613) 298-5021 dan.cudmore@gevernova.com | Ramana Relangi‡ Valmet Inc 3440Toringdon Way, Ste 300 Charlotte, NC Cell: 704-965-0411 ramana.relangi@valmet.com |
|  | Nick Folster‡ B&W Houston, TX 5059 FM 2920 Rd. Spring, TX 77388 Office: 281-405-6824 Cell: 207-974-6628 Cell: 207-974-6628 nbfolster@babcock.com |  |

‡ Denotes attendance in Fall 2026 meeting

PUBLICITY & NEWS RELEASE SUBCOMMITTEE

Nick Quigley - Chairman

FM

Johnston, RI

Cell: +1 401-480-7127
nicholas.quigley@fm.com

FIRE PROTECTION IN DIRECT CONTACT EVAPORATORS

AND ASSOCIATED EQUIPMENT SUBCOMMITTEE

‡Stephen Cox - Chairman

International Paper

6318 Highway 139

Bastrop, La 71220

Tel: 409-779-7104

Stephen.cox@ipaper.com

| ‡Aneeka Mahan – Vice Chair FM Property Insurance 2100 Reston Parkway; Suite 600; Reston, VA 20191 Tel: (703) 232-8087 aneeka.mahan@fm.com | Robert Orender Georgia Pacific 133 Peachtree Street NE Atlanta, GA 30303 Robert.orender@gapac.com | Robert Goddard XL Group 129 Drive 1143 Tupelo, MS 38804 Tel: 662 844-5897 robert.goddard@axaxl.com |
| --- | --- | --- |
|  |  | Joseph Lynch Swiss Re America Holding Corporation 1150 Sanctuary Parkway, Suite 425 Alpharetta, GA 30009 Tel: 1770-569-8706 Joe_Lynch@swissre.com |
| Mike McKenzie(new for spring 2024) International Paper Bogalusa Mill Tel: 19857328723 Michael.McKenzie1@ipaper.com | ‡Gerald “Trey” Nail (inducted in Fall 2024 with E&E becoming a member company) E & E Tech Cell: 662-633-9800 GNail@eandetech.com |  |

‡Denotes Attendance at the meeting in Fall 2025.

Did not meet In Fall 2026

INSTRUMENTATION SUBCOMMITTEE

Spring	2026 members

JC Browning, Jr (1998) – Chairman ‡

Georgia Pacific

133 Peachtree St. NE (30303) Atlanta, GA 30348-5605

Tel: 251-593-6254  john.browning@gapac.com

‡ Attended      New Member       Associate member

| Ben Bunner (2020) ‡ Vice-Chairman Andritz 5404 Windward Parkway, Suite 100W, Alpharetta, GA 30004 Cell: 678-907-7617 ben.bunner@andritz.com | C.A. Vossberg (<2000) ‡ Secretary Electron Machine Corp. P.O. Box 2349 Umatilla, FL 32784 Tel: 352-406-1351 ca@electronmachine.com | David T. Boudreau (2007) ‡ ISC RGP Document Controller SAPPI 1329 Waterville Road Skowhegan, ME 04976 Tel: 207-314-8024 dave.boudreau@sappi.com |
| --- | --- | --- |
| Gordon L. Vandenburg (2000) ‡ Liquid Solids Control, Inc. P.O.Box 259, Farm St. Upton, MA 01568 Tel: (603) 833-8536 gordie@liquidsolidscontrol.com | Andy Clement (2019) ‡ Fossil Power Systems 10 Mosher Drive P Dartmouth, Nova Scotia Canada B3B 1N5 Tel:902-468-2743 ext.245 clementa@fossil.ca | Joel Byrd (2015) International Paper Company 12515 Choctaw Rd Bogalusa, La 70427 Tel:985-516-1110 Joel.byrd@ipaper.com |
| Kevin Huelsbeck (2010) ‡ FM Global W4893 Cliff View Drive Sherwood, WI 54169 Cell: 920-205-5529 kevin.huelsbeck@fmglobal.com | Daniel Albert - (2019?) ‡ Rotork Mile Crossing Boulevard Rochester NY 67514624 (585) 247-2304 Daniel.Albert@Rotorq.com | Kevin Green ‡ Vaisala Inc. 3 van de Graaff Drive. Burlington, MA 01803 (P) 713-550-2534 Kevin.green@vaisala.com |
| Patrick Buyck (2024) SAPPI North America 2201 Avenue B, PO Box 511, Cloquet, MN 55720 Patrick.Buyck@sappi.com | Chris Clements (2024) Smurfit Westrock Chris.clements@westrock.co | Kyle Harper (2025) Georgia-Pacific 133 Peachtree St. NE (30303) Atlanta, GA 30348-5605d Kyle.Harper@GAPAC.com |
| Herman Haywood 2026‡ Domtar Herman.Haywood@domtar.com T 843.454.8954 C 910.280.9928 Marlboro Mill | Josh Crawford (2025) ‡ John H Carter Josh.Crawford@JohnHCarter.com Baton Rouge, LA | Ben Roberge (2025) ‡ Paragon Benrobergo@paragonconsults.com |
| Daniel Guarnieri (2024) SYLVAMO Rodovia SP 340 KM171 ¦ Mogi Guacu, SP, Brazil 13845-901 T: +55 19 3861-8972 daniel.guarnieri@sylvamo.com South Africa 4004 | Jari Sopanen (<2000) Jari Consultoria de Automacao Ltda, Avenida Frei Rogerio, 690 Centro, Curitibanos, Brazil 89520 Tel:+55 (47) 9 9672-2332 sopanenjari@outlook.com | Deshan Naidoo (2024) SAPPI 25 Heron Way Yellowwood Park Durban, South Africa 4004 Deshan.Naidoo@sappi.com |

‡ Denotes attendance in Fall 2026 meeting

PERSONNEL SAFETY SUBCOMMITTEE

Steve Morrison, Chairman‡

Georgia Pacific Corp.

Steve.morrison@gapac.com

TEAMs – (423) 516-6071

Cell – (423) 480-0119

| Sam Dean‡ Rayonier Advanced Materials 4470 Savannah Highway Jesup, GA 31545 Tel: (912) 427-5103 samuel.dean@ryam.com | Greg Sallee B&W Account Manager Mobile: 234-312-8388 cgsallee@babcok.com | Tom Edwards B&W twedwards@babcock.com |
| --- | --- | --- |
| Justin Helton Andritz +1 470-416-1342 justin.helton@andritz.com | Wayne Yenne‡ Fornax +1 719-338-6025 wayne.yenne@thefornax.com | Mathew Glenn Irving Pulp & Paper, Limited Recovery Superintendent P.O. Box 3007 408 Mill Street Saint John, New Brunswick Tel: (506) 634-4234 glenn.matthew@irvingpulp.com |
| Grey Gurkin International Paper International Paper Co. | Jake Dowland Georgia Pacific, LLC Power and Recovery Superintendent Brunswick Cellulose Mobile : (229) 202-4188 Jake.dowland@gapac.com | Francisco Britt FM One Cowboys Way Suite 600 Frisco, TX 75034 Tel: (972) 731-2145 Francisco.britt@fmglobal.com |
| Brook Holland Rayco Industrial 228 Wild Rose Lane Canton, NC 28716 Tel : (828) 421-0487 brook.holland@raycoindustrial.com |  |  |

‡Denotes attendance at the Fall 2026 meeting

MATERIALS & WELDING SUBCOMMITTEE

‡ Laura Nicol – Chair

Babcock & Wilcox

1200 E Market St, Ste 650

Akron, OH 44305

Cell: 330-361-0217

lsnicol@babcock.com

‡ this meeting

| Materials and Welding Committee Members |  |  |
| --- | --- | --- |
| ‡ William Burns Vice Chair ND Paper – Rumford Cell: 207-743-1029 William.Burns@us.ndpaper.com | *Maxime Simard FM Cell: (418) 435-1551 maxime.simard @fm.com *Alt: Andrew Bahnsen Andrew.bahnsen@fm.com * Alt: Jason Sirros ‡ | Scott Lowrie Andritz, Inc. Scott.Lowrie@andritz.com *Alt: Paul Ceravolo ‡ Cell: (678) 646-4198 Paul.Ceravolo@andritz.com |
| Brent Griffin Georgia-Pacific LLC Cell: (850) 910-1259 brent.griffin@gapac.com *Alt: Chad Harrod Cell: (404) 395-3064 Chad.Harrod@gapac.com | Jennings Bird Valmet Tel: 803 235 8091 Jennings.bird@valmet.com *Alt: Ron Reed ‡ Cell: (704) 281-3073 Ron.reed@valmet.com | Billy Collett – now at Legacy National Boiler Services, LLC. Cell: (423) 582-6958 bcollett@nationalboiler.com *Alt: No one from NBS present |
| Chris Rawls Applied Technical Services Cell: (757) 218-8465 crawls@atslab.com *Alt: Thomas Kapperman ‡ Cell: (678) 231-8025 tkapperman@atslab.com | Stacy Power ‡ Midstate SMS Tel: (843) 957-2111 Cell: (843) 297-1987 spower@msindustriealcorp.com *Alt: Chris Skorton ‡ cskorton@msindustrialcorp.com | James Hendrix ‡ IP – Pensacola Cell: (850) 516-8657 James.Hendrix@ipaper.com *Alt: Ben Coulter ‡ Ben.Coulter@ipaper.com (new alternate) |
| Jeremiah Yoder ‡ Lundberg Jansen Jeremiah.yoder@lundbergjansen.com Cell: (704) 408-6825 *Alt: | Jenny Joyce ‡ Legacy Boiler & Industrial Service Jenny.Joyce@legacyboiler.com Cell: (770) 616-3834 *Alt: Steve Harville ‡ |  |

SAFE FIRING OF BLACK LIQUOR SUBCOMMITTEE

‡Sarah Henke – Chair

Valmet

Tel: 919-454-3441

Sarah.henke@valmet.com

| Kurtis Barnette ND Paper Tel. Kurtis.barnette@us.ndpaper.com |  | Joel Byrd International Paper Tel: 85-516-1110 Joel.byrd@ipaper.com |
| --- | --- | --- |
| ‡ Nick Quigley FM Global Tel. 401-480-7127 Nickoles.quigley@fm.com | ‡Peter Donahue Fossil Power Systems, Inc. Tel: 902-468-2743, Ext. 251 Cell: 902-877-9312 donahuep@fossil.ca | ‡Len Erickson Power Specialist Assoc. Tel: 208-841-4246 len.erickson@PSAengineering.com |
| Jason Saulsbury Green Bay Packaging Tel: 902 908 0495 | ‡Wes Hill - Vice-Chair Georgia Pacific Tel 360-607-4189 ## Wes.hill@gapac.com | ‡Daniel Franco Recovery Specialist Cel: +57 3113001079 ## danielf721@gmail.com |
| ‡Guy Labonte FM Tel: 514-876-7412 Cell: 514-942-3651 ## guy.labonte@fm.com | ‡Doug Murch Smurfit Westrock Tel: 804-444-5245 Cell: 804-787-0781 douglas.murch@smurfitwestrock.com | ‡Alarick Tavares Smurfit Westrock Tel - 678 492-1107 ## alarick.tavares@smurfitwestrock.com |
| Mark Sargent Rayco Industrial Tel: 514-543-0480 ## Mark.sargent@raycoindustrial.com | ‡Pasi Miikkulainen Andritz p: +1 770 640 2414 m: +1 678 230 1525 Pasi.Miikkulainen@andritz.com | ‡ Brian Rawson International Paper Cell: 850-266-5259 brian.rawson@ipaper.com |
| Jason Lewis ND Paper m: 207-557-0952 ## Jason.lewis@us.ndpaper.com. | ‡Rudy Haraga – Fornax Services Tel: 860-268-1871 ## Rudy.haraga@thefornax.com | ‡Olli Kujanpaa – Georgia Pacific Tel: 404-432-8281 ## Olli.kujanpaa@gapac.com |
| Ryan P Henry Green Bay Packaging Inc. Tel: 501-306-8330 ## rhenry@gbp.com | ## ‡Keijo Pyorala Vaisala ## keijo.pyorala@vaisala.com | Jay Dilworth Pixelle Specialty Solutions Tel 717 225 4711 ## James.Dilworth@pixelle.com |
| Matthew Glen Irving Pulp and Paper ## glenn.matthew@irvingpulp.com | ## ‡Evangelos Townsend ## B&W ## Office: 281-405-6825 ## Mobile: 469-815-8395 ## Emtownsend@babcock.com |  |

‡Denotes attendance at the meeting in Fall of 2026.

No new members

WASTE STREAMS SUBCOMMITTEE

### Paul Seefeld – Chairman *

LundbergJansen Technologies

9246 Audubon Park Ln S

Jacksonville, FL 32257

Cell: 904-614-6492

### Paul.seefeld@lundbergjansen.com

| Abby George* Valmet 3440 Toringdon Way, Bldg 3, Suite 300 Charlotte, NC 28277 Tel: 252-308-5330 Abby.George@valmet.com | ## Neil Chaudhuri* FM 100 New Park Place, Suite 200 Vaughan ON Canada L4K OH9 Tel: 647-894-5680 Neil.chaudhuri@fmglobal.com | Nicole Crawley* International Paper Pensacola, FL Nicole.Crawley@ipaper.com |
| --- | --- | --- |
| Cobb Golson SmurfitWestrock St. Augustine, FL Tel: 904-826-7430 Cobb.golson@smurfitwestrock.com | John Lewis* Fluor 100 Fluor Daniel Drive Greenville, SC 29607-2762 Tel: 864 517-1683 john.lewis@fluorgov.com | Greg Swayne* Andritz 5405 Windward Parkway Alpharetta, GA 30004 Cell: greg.swayne@andritz.com |
|  | Wayne Bucher* NORAM Birmingham, AL Wayne.bucher@gmail.com | Greg Wass LundbergJansen 8271 154th Ave NE Redmond, WA 98052 Tel: 425-283-5070 greg.wass@lundbergjansen.com |
| Kevin Sapp – Vice Chairman* Georgia Pacific Atlanta, GA Tel: 387-227-1038 Kevin.sapp@gapac.com |  |  |
|  |  | . |

*Denotes attendance

Did not meet In the Fall of 2026

WATER TREATMENT SUBCOMMITTEE

Fall 2026

‡Tom Przybylski

Power Specialists Assoc. Inc.

### tom.przybylski@psaengineering.com

| ‡Jeff Armstrong Solenis ### E-mail Address jarmstrong@solenis.com | Rick Baxter Rayco ### E-mail Address richard.baxter@raycoindustrial.com | Michael Bayse George H. Bodman, Inc. ### E-mail Address bbayse@aol.com (Substitute: Gene Cotton) |
| --- | --- | --- |
| ‡Fred Call Buckman ### E-mail Address fccall@buckman.com | ‡Frank Crumpler Nalco ### E-mail Address fcrumpler@ecolab.com alternate: Jim Gannon | ‡Cam Davies AON ### E-mail Address cameron.davies@aon.ca |
| ‡Frank Destefano 3D ### E-mail Address DestefanoFrank55@gmail.com | Don Downey Purolite ### E-mail Address don.downey@purolite.com | Peter Fogg Georgia Pacific ### E-mail Address peter.fogg@gpac.com |
|  | Nick Wildey Georgia Pacific ### E-mail Address nicholas.wildey@gpac.com | Tom Meehan FM Global ### E-mail Address thomas.meehan@fmglobal.com |
|  | Dylan Price Rayco ### E-mail Address dylan.price@raycoindustrial.com | ‡Dave Tjaarda WestRock ### E-mail Address dave.tjaarda@smurfitwestrock.com |

‡ = Denotes attendance at meeting  Fall 2026

- Denotes new subcommittee member on this list; previously added to subcommittee.

Registration List*

BLRBAC Fall 2026 Meeting - Registrations       Total -224

| First Name | Last Name | Company |
| --- | --- | --- |
| Frank | DeStefano | 3D Team |
| Victor Porter | Pyszynski | 3S TEAM, LLC |
| David | Dunn | Acuren Inspection |
| Catherine | Noble | Acuren Inspection |
| Wayne | Grilliot | AF&PA |
| Rick | McRae | Alabama Laser |
| Sai | Mudiam | Alabama Laser |
| Ryan | Weathey | Alabama river cellulose |
| Greg | Imig | Andritz |
| Samuel | Miller | Andritz |
| Lucy | Moore | Andritz |
| John | Phillips | Andritz |
| Gregory | Swayne | Andritz |
| Brandon | Hamilton | Andritz Inc |
| Niilo | Kostiander | Andritz Inc |
| Daniel | Villanueva | Andritz Inc |
| Paul | Ceravolo | Andritz Inc. |
| Pablo | Corvalan | Andritz Inc. |
| Pasi | Miikkulainen | Andritz Inc. |
| Ben | Bunner | Andritz, Inc. |
| Cameron | Davies | Aon |
| James | Franks | AXA XL Risk Consulting |
| Jeff | McCartney | B&W |
| Nick | Folster | Babcock & Wilcox |
| Paul | Griffin | Babcock & Wilcox |
| Laura | Nicol | Babcock & Wilcox |
| Greg | Sallee | Babcock & Wilcox |
| Kawmae | Sawyer | Babcock & Wilcox |
| Evangelos | Townsend | Babcock & Wilcox |
| Brett | Gushue | Babcock & Wilcox FPS Inc |
| Dean | Clay | BSI |
| Francis | Navojosky | BSI - Boiler Services and Inspection |
| Fred | Call | Buckman |
| Olson | Cannon | Buckman |
| Jonathan | Byers | C&H Industrial Services |
| Zane | Cradic | C&H Industrial Services |
| Thomas | French | Clearwater Paper |
| Casey | Garland | Clearwater Paper |
| Steven | Parnell | Clearwater Paper |
| Dion | Smith | Clearwater Paper |
| Kristopher | Waide | Clearwater Paper |
| Wayne | Bunce | Clearwater Paper Corporation |
| Ishaq | Jameel | Clyde Industries |
| Wanicley | Viana | CMPC |
| James | Biggs | Crenshaw Machine Systems |
| Juan | Reyes | Crenshaw Machine Systems |
| Nico | Ferretti | Diamond Power |
| Matt | Saunders | Diamond Power |
| Kelli | Tucker | Diamond Power |
| Simon | Youssef | Diamond Power |
| Khalid | Abdulsalam | Diamond Power International, LLC |
| Gregory | Burns | Domtar Corporation |
| Herman | Haywood | Domtar Paper |
| Ryan | Smith | E and E Tech |
| Gerald | Nail | E&E Tech |
| Blake | Hallam | Electron Machine Corporation |
| Brad | Osborne | Electron Machine Corporation |
| C.A. | Vossberg | Electron Machine Corporation |
| Martin | Senechal | Enero Solutions |
| Steven | Moore | Envision-MC Group, LLC |
| Resham | Adhikari | FM |
| Shafia | Ahmad | FM |
| James | Beckham | FM |
| Neil | Chaudhuri | FM |
| Scott | Crysel | FM |
| James | Gibbs | FM |
| Derrick | Gossen | FM |
| Wayne | Hatch | FM |
| Guy | Labonte | FM |
| Jimmy | Onstead | FM |
| Nicholas | Quigley | FM |
| Richard | Sherwin | FM |
| Jason | Sirros | FM |
| Vincent | Tremblay | FM |
| Rudy | Haraga | FORNAX Services, LLC |
| Wayne | Yenne | FORNAX Services, LLC |
| Andy | Clement | FPS |
| Peter | Donahue | FPS |
| Austin | Starnes | GCF |
| Chris | Thomas | GCF - Columbus Mill |
| Matt | Hill | GCF Columbus Mill |
| Drew | Parish | GCF Columbus Mill |
| Daniel | Krekeler | GCFibers |
| Michael | Rushing | GE Steam Power |
| Dan | Cudmore | GE Vernova |
| John | Lewis | GE Vernova |
| Jason | Shaw | GE Vernova |
| Yoram | Schaker | GE Vernova - Steam Power |
| Bailey | Anderson | Georgia Pacific |
| Rickey | Bazelle | Georgia Pacific |
| ETHAN | BLAIR | Georgia pacific |
| JC | Browning | Georgia Pacific |
| Cory | Carter | Georgia Pacific |
| Olli | Kujanpaa | Georgia Pacific |
| Justice | Mallett | Georgia Pacific |
| Adam | Marickovich | Georgia Pacific |
| Tom | Meadows | Georgia Pacific |
| Steve | Morrison | Georgia Pacific |
| Robert | Orender | Georgia Pacific |
| Jackson | Reid | Georgia Pacific |
| Austin | Rozek | Georgia Pacific |
| Avery | Farrish | Georgia Pacific Brunswick Cellulose |
| Greg | Zavadoski | Georgia Pacific, LLC |
| Wes | Hill | Georgia-Pacific |
| Gregg | Lentz | Georgia-Pacific |
| Michael | Roberts | Georiga Pacific |
| Mark | Dufault | Global Cellulose Fibers |
| Mike | Kindlan | Global Cellulose Fibers |
| Boyd | Hilton | GP Brunswick |
| Jody | Nichols | High Temperature Technologies |
| Rob | Delp | Integrated Global Services (IGS) |
| Ben | Coulter | International Paper |
| David | Frazier | International Paper |
| James | Hendrix | International Paper |
| Rick | Kriner | International Paper |
| Brian | Rawson | International Paper |
| Nicole | Crawley | International Paper - Pensacola Mill |
| Kevin | Sarver | International Paper - Riverdale Mill |
| Marcus | Mahan | IP |
| Joshua | Crawford | John H. Carter |
| Jerrel Bobby | Johnston | Johnston Construction LLC |
| Michael | Gareri | Kraft Powercon |
| Derek | Godbold | Kraftpowercon |
| Billy | Collett | Legacy Boiler & Industrial Service LLC |
| Steve | Harville | Legacy Boiler & Industrial Service LLC |
| Jenny | Joyce | Legacy Boiler & Industrial Service LLC |
| William | Patterson | Legacy Boiler & Industrial Service LLC |
| Donnie | Wilson | LEGACY BOILER AND INDUSTRIAL LLC |
| Gordon | Vandenburg | Liquid Solids Control, Inc. |
| Jonathan | Starling | Liquidmetal Industrial Solutions |
| Mark | McCabe | Lundberg Jansen Technologies |
| Nicole | Brister | Lundberg Jansen Technologies, Inc. |
| Morgan | Silverman | Lundberg Jansen Technologies, Inc. |
| Jeremiah | Yoder | Lundberg Jansen Technologies, Inc. |
| Paul | Seefeld | LundbergJansen |
| Christopher | Schutter | Metso |
| Robert | Richards | Metso USA Inc. |
| Stacy | Power | MidState SMS |
| Roger | Lawton | Milhous Company |
| Jason | English | Ml ball |
| Frank | Crumpler | Nalco |
| William | Burns | ND Paper |
| Wayne | Bucher | Noram Engineers |
| Jon | Foan | Noram Engineers |
| Paul | Leanza | NWL |
| Derrick | Naidoo | OJI Fibre Solutions - Kinleith Mill |
| Travis | Jackson | Packaging corp of america |
| Tell | Hunt | Packaging Corporation of America |
| Christina | Karas | Packaging Corporation of America |
| Boyd | Nelson | Packaging Corporation of America |
| Carter | Cameron | PCA |
| Cory | Olds | PCA |
| Lauren | Sheffield | PCA |
| Grant | Williams | PCA |
| Brett | Elgin | Pixelle Specialty Solutions |
| Anna | Racine | Pixelle Specialty Solutions |
| Tom | Przybylski | Power Specialists Assoc. |
| Leonard | Erickson | Power Specialists Associates |
| Daniel | Lishbrook | Power Specialists Associates |
| Vince | Barreto | PowerPlus Cleaning Systems |
| Carl | Wise | PowerPlus Cleaning Systems |
| Nathan | Herrington | ProcessBarron |
| Jen | Little | ProcessBarron |
| Derek | McCallum | ProcessBarron |
| Jennifer | Smith | ProcessBarron |
| Tripp | Whatley | ProcessBarron |
| Thomas | Kapperman | Project Services LLC |
| Daniel | Franco | Retired |
| Daniel | Albert | Rotork |
| Morgan | Brumfield | RYAM |
| Sam | Dean | RYAM |
| David | Boudreau | Sappi North America |
| Justin | Carr | SEI |
| Bernie | Abramczyk | SEI-Group |
| Andrew | Jones | SHB Power Plant Engineering |
| Benjamin | Roberge | Sigma 7 |
| Christian | Cote | Sigma7 Risk Engineering |
| Chris | Skorton | SMS Mid-State |
| Dylan | Brooks | Smurfit Westrock |
| Aubrey | Brunson | Smurfit Westrock |
| Harley | Carter | Smurfit Westrock |
| Joe | DeRoy | Smurfit Westrock |
| Jimmy | Hicks | Smurfit westrock |
| Jeremy | Hooper | Smurfit Westrock |
| Scott | Moyer | Smurfit Westrock |
| Douglas | Murch | Smurfit Westrock |
| Ian | Owen | Smurfit Westrock |
| Cameron | Pate | Smurfit Westrock |
| Sébastien | Pronovost | Smurfit Westrock |
| Alarick | Tavares | Smurfit Westrock |
| David | Tjaarda | Smurfit Westrock |
| K W | Urquart | Smurfit Westrock |
| Wade | Shirley | Smurfitwestrock |
| Stéphane | Bouchard | Smurfit-Westrock |
| Jeff | Armstrong | Solenis |
| Anton | Vermaak | Solenis |
| Akseli Pietari | Kaakko | SouthE Inc. |
| Patrick | Griffin | Southern Environmental Inc |
| Todd | Grave | Sullivan Higgins and Brion Power Plant Engineering |
| Michael | Bruce | Sylvamo |
| Caleb | Martin | Sylvamo |
| Jamie | Osborne | Sylvamo |
| Kristi | Schlicksup | Sylvamo |
| Taylor | Sease | Sylvamo |
| Linda | Trinh | Sylvamo |
| Ronald | Pon | The Babcock & Wilcox Company |
| Kevin | Green | Vaisala |
| Keijo | Pyorala | Vaisala |
| Travis | Conner | Valmet |
| Abby | George | Valmet |
| Rob | Goggins | Valmet |
| Oscar | Guevara | Valmet |
| Sarah | Henke | Valmet |
| Daniel | Morrison | Valmet |
| Steve | Newton | Valmet |
| Chris | Presutti | Valmet Inc |
| Ramana | Relangi | Valmet Inc |
| Ronald Joseph | Reed Jr | VALMET INC. |
| Mikko | Anttila | Valmet Technologies Oy |
| Jonas | Gestranius | Valmet Technologies Oy |
| Sammy | Wiggins | Westrock mahrt mill |
| John | Harris | WSI |
| Ivan | Burdin | WSI U.S. LLC |
| Blair | Carter | Zurich Resilience Solutions |

MAIN COMMITTEE MEETING

- Introduction – (Gregory Burns – Chairman)

Good morning!  Welcome to the Fall 2026 BLRBAC Main Committee Meeting!  Thank you all for being here and participating this week.  It is hard to believe but this is our 5th meeting at the Atlanta Airport Hilton Hotel, and I hope everyone finds things to their satisfaction and made use of their voucher provided by BLRBAC.  With tax and tip that just about covers breakfast here at the hotel. As always please share any issues good or bad with your experiences here at the Hilton.  We will continue to work with the Hilton Hotel to close any gaps.  The hotel was still charging some deposit fees.  I know I was charged $299.  The EC is working to resolve this issue going forward.

I think we had a good week with a lot of excellent participation, especially in the subcommittee meetings, which were well attended.  We had 224 registered attendees compared with 223 during the Fall 2025 meeting.  BLRBAC has thrived over the years from its face-to-face interactions at these meetings.  A lot of discussions and exchange of good information.  We continue to build momentum on our BLRBAC meeting participation.  This week’s meeting had a very good turnout.  The continued good turn makes it possible for us to keep our rates low.  Still at $400 and provide that $30 voucher mentioned earlier.

With that we will carry on with our business.  The Main Committee Meeting is now officially open.  This meeting is being held in strict compliance with BLRBAC’s Anti-Trust Policy.

PLEASE REMEMBER THAT ALL BLRBAC MAIN AND SUBCOMMITTEE MEETINGS INCLUDING THIS SESSION ARE TO BE HELD IN STRICT COMPLAINCE WITH THE BLRBAC ANTITRUST POLICY.  DISCUSSIONS INVOLVING PRICE, PRICING POLICY, AND ANY RESTRAINT ON COMPETION ARE NOT ALLOWED DURING THESE MEETINGS.

I’ve reviewed the registration list and found that we have voting members from 16 of 26 Regular Member companies at this meeting.  That is 62% of regular member companies in attendance and therefore, I am declaring that we have a quorum for today’s Main Committee meeting.

We will begin with some introductions from the executive committee members this morning.  We will introduce ourselves one-by-one.  I will kick it off, I am Gregory Burns Executive Committee Chairman and I am the Director for Power and Recovery for Domtar,

Dave Tjaarda – Vice-Chairman – Smurfit WestRock

Scott Moyer – Operating Companies rep – Smurfit WestRock

Daniel Franco – Secretary – Retired Consultant

Brad Osborne – Treasurer – Electron Machine Corporation

Ev Townsend – Manufactures rep – Babcock & Wilcox

Jimmy Onstead – Insurance rep – Factory Mutual

- Old Business - (Gregory Burns)

ACCEPTANCE OF THE FALL2024 MEETING MINUTES –

Next, we will move into old business and accept the Spring 2026 meeting minutes. The     Meeting Minutes for the Spring 2026 BLRBAC session have been posted on the BLRBAC web site.  The website is blrbac.net.  Do any members have any comments or discussion points regarding the Spring 2026 BLRBAC meeting minutes as posted?

Can I get a motion to accept the Minutes as posted?  We have a motion.  Second?  All in favor of accepting the minutes as posted.  Anybody opposed?   Thank You! The Spring 2026 Meeting Minutes have been approved.  There was no other old business to discuss.

- New Business Report - (Gregory Burns / Daniel Franco)

Next, we will move to new business.

In accordance with the BLRBAC Articles of Association and By-Laws Term of Officers: The Chairman and the Vice-Chairman shall be elected biannually from among the representatives of the Regular members. They shall serve until the next appropriate Annual Meeting of the members or until their successors are elected.

The Chairman and Vice-Chairman shall not serve more than two consecutive two-year terms.

Not less than 30 nor more than 60 days before the appropriate annual meeting of BLRBAC, the Chairman shall appoint a Nominating Committee of three persons. The Nominating Committee shall report to the annual meeting a slate of candidates for Chairman, Vice-Chairman, and the other members of the Executive Committee.

In compliance with the Articles of Association the Executive Committee chairperson nominated Robert Orender from Georgia Pacific, Sarah Henke from Valmet and Scott Crysel from FM for the nominating committee.  The Executive Committee, with the exception of Scott Moyer, who is the Operating Company Representative, expressed their desire to remain as committee members.

The Nominating Committee met to develop the slate of candidates to be put to vote today. Scott, could you come up to the podium to deliver your slate of candidates for vote.

{Scott Crysel presented the list of candidates and then put them to a vote for the regular membership}

The list of candidates was as follows:

Chairperson – Gregory Burns

Vice Chairperson - Dave Tjaarda

Operating Company Rep - Steve Morrison – (New)

Insurance Representative - Jimmy Onstead

Manufacturer’s Representative - Ev Townsend

Secretary* - Daniel Franco

Treasurer* - Brad Osborne

We will now put the proposed slate of Executive Committee candidates to a vote.  Could all voting regular member representatives please stand?  All in favor of approving the slate of candidates. Any opposed?  Let it be noted that the list of Executive Committee candidates has been approved.

- Executive Committee Report - (Gregory Burns)

The executive committee met in a closed session at 4PM on Tuesday.

- Meeting started at 4PM with all members in attendance.

- The EC reviewed BLRBAC Financial status and preliminary results to which will be covered in the Treasurers report.  BLRBAC is sound financially.

- The Executive Committee discussed the make-up of the Executive Committee and that we should try to ensure the committee is as diversified among member companies as possible.

- Gregory Burns discussed the Nominating Committee that he enlisted in accordance with the BLRBAC Articles of Association and By-Laws

  - Rob Orender (GP), Sarah Henke (Valmet), & Scott Crysel (FM).  The Nominating Committee did a thorough analysis looking at subcommittee participation and attendance going back at least 10 years to determine their nomination.

  - The NC plans to present the current board members as the slate of candidates except for Scott Moyer.

  - The NC reported that they will propose Steve Morrison (GP) as the Operating Company representative.

- Hotel

  - Hotel still charging deposit of $299.  We will need to clarify why this is being charged and ensure the hotel takes the proper precautions, so it does not repeat itself again.

  - Hotel website is still hit or miss.  This may be related to the $299 charges as many people register on the main Hilton website using the group code.

  - Material and Welding subcommittee had round tables and a tiny monitor.  The solution may be for the Executive Committee to inspect rooms on Sunday night as they are being put together.  Some of the Executive Committee are at the hotel in the early afternoon on Sunday so this may not be much of an issue.

- Changes to subcommittee chairs

  - Scott Moyer was nominated by the ESP subcommittee to chair the ESP subcommittee.  The EC voted and approved Scott with Scott Moyer abstaining from voting.

- Membership update - New Members (Daniel Franco) – Rebuilding membership continues.

  - No new regular members have been added since the Spring 2026 meeting.

- Meeting updates

  - Metroconnections.  We discussed MetroConnections and they work they are doing.  The consensus was that MetroConnections is doing good work, are responsive to our demands and that the reduced on-site schedule started during the spring was working just fine.

  - The question of whether committees should be required to meet at least once during every meeting (other than the Fire in DCE committee) was asked by Gregory Burns.

    - Should Subcommittees fill empty time with presentations similar to what the Materials and Welding subcommittee has been doing.

    - The consensus of the EC was that we wouldn’t make any changes to how the subcommittees manage their sessions at this time.

- The EC discussed how we can improve the turnout for the Activity Night.  Some vendors expressed concern that non-Activity Night vendors were taking members out on Tuesday night.  There has been a long-unwritten rule that vendors do not do that.

- Service awards –

  - Only one service award was to be given during the main committee meeting and that was to Frank Navojosky.  We decided Scott Moyer, his replacement on the ESP Subcommittee, should present the award.

  - No names were suggested for Spring 2027 service awards.

- The EC discussed the approval of documents under review that the membership will be voting on during the main committee meeting.  No new issues were raised with the documents, and the vote would proceed as planned.

  - Instrumentation and controls

  - Emergency Shutdown Procedures

  - Waste Streams

- The EC discussed the approval of documents for the Spring 2027 meetings.  There appear to be four up for a vote.  The EC has been in communication with the Safe Firing of Black Liquor and the Auxiliary Fuels subcommittees on the proposed changes and believes most issues have been resolved.  These

  - Safe Firing of Black Liquor

  - Auxiliary Fuels

  - Material and Welding

  - Personnel Safety

- We discussed BLRBAC regular membership and how to handle operating companies that do not submit incident reports as a matter of policy.  Analysis, classification and reporting of incidents is BLRBAC’s primary function.  Possible alternatives are to allow these companies to participate as associate or non-voting members.  They would still be able to attend meetings and participate in subcommittees but not vote.  No decision was made and the subject was shelved.

- The meeting adjourned at 5:30 PM.

5.0 Treasurer’s Report (Brad Osborne)

As of October 06, 2026, the balance in our checking account was $185,798.81. After the reduction in cost and the added amenities we still added $7,000 to the bank balance from the Spring meeting. The Fall 26 meeting had 187 advanced registrations; there were 37 at-door registrations for a total of 224. Our estimated gross meeting revenue for this meeting is $90,550. Our estimated expenses for the Fall meeting are 55,000 to the hotel and $25,000 to Metro, there will also be a few admin fees we need to account for such as legal reserves and secretarial work. We paid $28,000 to the hotel before the meeting. The goal of the Fall 26 meeting budget was to try and break even and keep the bank balance at current levels.

Participation was the same as the Fall 2025 meeting and slightly up from the spring 2026 which is normal. There were 24 attendees from outside the US. With 17 people from Canada, 2 from New Zeeland, 3 from Finland, 1 from Brazil, 1 from Colombia.

We will be in the Hilton again for the next two meetings. The committee continues to evaluate the bank balance and conference costs; for this meeting we kept the price of the conference the same as the spring and continued to provide the extra amenities that hopefully added some extra value to attendees. The goal of EC is to maintain a bank balance that covers at minimum one complete meeting, an appropriate legal reserve and all other expenses that may arise. I do not see any reason to raise conference costs for the Spring of 2027.

| Balance as of October 6th, 2026 | $185,798.81 |
| --- | --- |
| Estimated Spring Gross Meeting Revenue | $90,550 |
| Estimated Expenses for Spring | $89,300 |
| Fall Meeting Hilton and AV | $ 55,000.00 |
| Metroconnections | $25,000 |
| ESP | $ 3,500.00 |
| Office | $ 800.00 |
| Other Expenses from Budget | $5,000 |
| Total | $89,300 |
| Estimated Meeting Revenue | $1,250 |
| Prepayment | $28,000 |
| Estimated EOM Checking Balance | $ 177,828 |

6.0  Secretary’s Report - (Daniel Franco)

As explained before we continue to build the membership list.

7.0 SUBCOMMITTEE REPORTS

7.1	AUXILIARY FUEL – Adam Marickovich (Georgia Pacific)

BLRBAC Spring Meeting Aux Fuels Committee

10-5-2026

Meeting was opened at 1:00 PM

The Aux Fuels committee met in the afternoon to review and incorporate comments received from the Executive Committee on the Aux Fuel Document

Anti-Trust was read

Meeting Guidelines were reviewed

Introductions:

4 Members

Adam Marickovich – adam.marickovich1@gapac.com

Derrick Gossen – derrick.gossen@fm.com

Greg Imig – greg.imig@andritz.com

John Lewis – john.c.lewis@gevernova.com

5 Guests

Taylor Sease (Joined as new member) - taylor.sease@sylvamo.com

Christina Karas – ChristinaKaras@packagingcorp.com

Caleb Martin – Caleb.martin@sylvamo.com

Niilo Kostiander –Niilo.Kostiander@andritz.com

Neil Chaudhuri – Neil.chaudhuri@FM.com

- The committee would like to move to a 3-5 year update schedule of our document after updating the current document.

- Discussed document changes:

  - Safety System Override (SSO) vs Jumper Log discussion. Jumper log is everything both physical and non-physical jumpers and bypasses changes.

  - Remote light-off of aux burners. Visual inspection to determine if burners are going to function properly by having a clear path into the furnace.

  - OEM recommended firing range to be standardized for ignitor pressures.

  - 6.1.14 – What process is in place to extend an annual outage beyond 12 months. Insurance providers have standards/procedures for this.

  - 6.1.15 – Changed to follow comments.

  - The committee discussed the tripping the precipitator and developed working to make this an optional consideration.  Wording was made similar to the ESP document.

  - The committee discussed the Major Maintenance Outage comment from the executive committee asking for more details on what is required to receive approval to extend beyond 12 months.  The Aux fuel committee did not think that type of prescriptive wording belonged in their document.

Meeting was closed at 3:00 PM.

7.2 ESP SUBCOMMITTEE REPORT – Frank Navojosky (BSI)

ESP Report out to BLRBAC Executive meeting   10/7/26

Closed Meeting opened at 8:00 AM 10/5/26

Call to Order – Reviewed Antitrust Slide

Membership attendance

We had 12 members present out of 14 active members in the closed meeting with 1 absent. (Angelo Porchetta of WCBLRBAC Jason Shaw attended as his Alternate). Mike Bruce cancelled last minute

For a total of 13 people in attendance

Voted in Nick Folster as replacement for John DeFusco of B&W

Frank Navojosky resigned as Chairman. Vice Chair Scott Moyer will take over as Chair subject to EC approval. Vice chair will be decided

Regular Business

Reviewed and Approved the Previous Minutes – April 6th, 2026

Reviewed 21 Total incidents reported (19 US and Canada and 2 international)

0 Smelt Water Explosions

0 ESP with no leak

0 Smelt leak

1 DT Incident (1 explosion)

14 Non-critical

3 Critical

3 Critical Pressure part incidents (All in Operation)

6 Incidents ESP’d (2 Gen bank and 1 Floor, 1 Spout wall lower header, 1 Penthouse, 1 U-Furnace)

3 Critical incidents occurred with a bed in the boiler

3 Critical with a bed in the boiler and ESP’d

0 Critical with a bed in the boiler and not ESP’d

100% ESP’d that should have ESP’d.

Root causes (Mechanical damage and Operator error may be related to experience issues?)

1 Thinning

2 Fatigue

1 Thermal Fatigue

5 SAC/SCC

2 Mechanical damage

6 Weld failure

We have continued to encourage reports of near misses/smelt rushes with DT’s, 1 considered an explosion.

Frank Navojosky and Mike Bruce updated Dean’s multi-year lessons learned document on the BLRBAC website and it has been updated on the website.

We finalized changes to our latest ESP Guideline Document and it was posted for comment to be voted on in Wednesday’s meeting.

We discussed the need to automate SCAH condensate isolation on ESP or not. We decided that the check valves are sufficient protection for condensate backflow and need to be maintained. A best practice would be such that if the condensate removal discharge ties into a common system that could be back pressured, then a routing check valve inspection should be instituted.

We discussed the need to activate Large Tube Leak Logic on all low drum level trips or not. The ESP subcommittee agree that Activating Large Leak Logic on low drum trip alone makes sense and agrees that instituting it would be beneficial. The ESP subcommittee would like to review the wording of the SFBL subcommittee guideline.

Meeting Adjourned at 3:15 PM 10/5/26

Please check Appendix I for the incidents discussed in this meeting and Appendix II for the ESP Presentation.

The revised ESP Guidelines have been posted for review on the BLRBAC website for at least the minimum of 60 days as required by the BLRBAC operating procedures and bylaws.  We will now put the revised guidelines to a vote.  Could all voting regular member representatives please stand?  All in favor of approving the revised ESP guidelines. Any opposed?  Let it be noted that the revised ESP guidelines have been approved.

7.3      FIRE PROTECTION IN DIRECT CONTACT EVAPORATORS-Stephen Cox

Did not meet Fall of 2026

7.4	INSTRUMENTATION – John Browning (Georgia Pacific)

Fall 2026 ISC meeting minutes

- Review BLRBAC anti-trust statement.

- Introductions and committee roll call, establish Quorum

- ISC committee members -17,  visitors-18

  - Morning members attending 12 Quorum achieved? Yes   No

  - Afternoon members attending 9 Quorum achieved? Yes   No

- Review: Spring 2026 Minutes / Approved.

- New members: Avery Farrish with Georgia Pacific, Linda Trinh with Sylvamo, Matthew Hill with GCF. Leaving member Sara Pritchard GP.

Old business:

- CA Vossberg to meet with SFBL @ 10:30 and present some suggested changes to Chapter 4 and Chapter 6 for refractometers to read less than or equal to off-line solids tests. Refract ISC request to SFBL Fall 2026 100126 jcb

- Review status of posted documents.

New Business:

Brent Bourassa with Clearwater Paper submitted: ISC RGP document Page 6:  While we agree 	that ESP should not be in the BMS, the comment about fail safe is misleading.

Fail safe or Fail state for ESP devices is the state a valve or other output device goes to, typically open, closed or last state.  Recommend entire paragraph in parentheses be struck. And replaced with: ESP (Emergency Shutdown Procedure) systems should be configured with Fail-Safe mode of not initiating ESP actions.  ESP should not be incorporated / reside in new BMSs because ESP should not depend on BMS system functioning correctly.

An ESP system’s protective functions are to remove fuels and drain the boiler.  A Fail-Safe configuration for ESP functions would have all drain valves fail open, all steam and water supplies fail closed on a system failure.  This is why the ESP system, and functions should be configured “Fail-Last” position. This failure mode is also the driver for a “Secondary Means” of performing an ESP.  This way, if I am not in an ESP, nothing will happen. If I am in an ESP, it will continue. However, I agree the statements you mentioned needs additional clarification.

From Greg Burns: I agree with John Browning and the current verbiage on this topic.

Page 8: Same thing: “The esp should not be configured fail safe” Yes, it should be configured fail safe, specifically, ESP should be configured to keep rapid drain valves closed during failed power, air or communication conditions.

Recommend rephrase:  Note:  ESP (Emergency Shutdown Procedure) systems should be configured with fail safe mode of not initiating ESP actions.  ESP should not be incorporated/reside in new BMSs because ESP should not depend on BMS system functioning correctly.

Page 10: Same: Recommend rephrase Rather than “The exception .. requirement” with

The exception to this is the ESP system, which should not initiate ESP actions, or change ESP outputs based on failed communication. Communications that are critical to the safe operation of any of the BMS shall be configured Fail-Safe or use a heartbeat / watchdog configuration to ensure the communications link is active. The exception to this is the ESP systems that are not configured fail-safe due to the power to initiate and hold last position design requirement.

Page 14: Same Recommend rephrase

Note:  ESP (Emergency Shutdown Procedure) systems should be configured with fail safe mode of not initiating ESP actions.  ESP should not be incorporated/reside in new BMSs because ESP should not depend on BMS system functioning correctly. Note: ESP (Emergency Shutdown Procedure) systems should not be configured Fail-Safe and should not be incorporated / reside in new BMSs due to conflicting failure modes.

Page 16:  Rephrase: MFT relay and circuit shall be designed so that on loss of power or circuit interruption, the MFT relay coil deenergizes and contacts fail open.  This fail-safe condition must result in no fuel added to boiler. MFT relay and circuit shall be designed Fail Safe. On loss of power or circuit interruption, the MFT relay coil deenergizes and contacts must fail open.

Scott Crysel with FM global submitted:

In the instrumentation and controls checklist:

B.9 Should be steam and not feedwater supply that is stopped. Corrected in latest revision.

Question: Our steam coil air heater systems have condensate valves that are also driven                                        closed on ESP initiation, should this be included? Same for the feedwater systems, I would              assume they have an outlet valve that would have to be closed.

Question to ESP committee, - Should control valves associated with block valves be closed on ESP i.e. indirect liquor heater, feedwater valve.

Sent to Greg B and Scott M:

I received the above question from Scott Cyrsel with FM global concerning our guidance table: (not sure what feedwater systems he is referring to).

I feel this should come from the ESP committee. My POV is I don’t want anything back feeding from the condensate system but also concerned if I bottle the system up and the supply block valve fails to close.

We should be able to take up that question if it is not covered already and Scott Crysel is on the ESP Subcommittee.  The way the ESP document reads, it could be implied that a mill would shut all remote operated valves for the steam coil air heaters whether steam or condensate.  I don’t think that you would want to close any valves between the SCAH and the condensate tank as we would want that system to drain condensate that may accumulate.  There should be check valves in those lines to prevent condensate back flow.

Should check valves be required in systems that could back feed pressure?

C.2   Remove two first outs, add “First out Feature for High pressure MFT”

- And “First out Feature for Low pressure MFT”. Agreed

E. 1   Excess Capital letter in title. Agreed

G. 28 Permissive:  Cannot initiate liquor header purge during Manual Back Liquor trip.  (if that is what they meant, alternative Permissive: Cannot initiate Manual Black Liquor Trip during liquor header purge. ((I doubt this is correct)) Agreed, we need to remove a liquor header purge as a permissive for a Black liquor divert

Inside of the document you list ISC by itself for the reference, I believe the intent is that it refers to the Instrument sub-committee's main document, can you somehow note in the checklist reference ISC refers to the main sub-committee document: Guidelines for the Design, Installation, and Operation of Recovery Boiler Process Control, Safety System (BMS), and Emergency Shutdown Procedure (ESP) system or change the reference to the document name and revision similar to the others coming from safe firing of black liquor etc. The items listed with the ISC reference are those we could not find in any other RGPs. Due to being in the document for years, instead of just removing them, we left them in the table with the ISC reference.

In the ESP document, we state that the feedwater control valve should not be relied on and that a stop valve is required. Based on this, should closing the control valve be considered a Class II? Concerning closing the feedwater control valve, we recommend closing any supply control valve associated with a stop valve due to the possibility of stop valve failure to close.

Also, in my opinion, position feedback for the FW stop valve is critical info for the operator.  Why would the “open” position not be a Class I?

The feedwater stop valve proven closed is critical to verify position during an ESP, if not proven closed then the system should be manually isolated, while proven open is more an operational status.

Should this not be “ESP closes steam supply to air heater”? Agreed, changed

A stuck sootblower is a critical failure.  Why are a failure to retract alarm and a high steam flow alarm not considered a Class I? Unfortunately, the only guidance for soot blowers in the other RGPs are as shown, trip steam and retract on an MFT and ESP. That said, I am not in disagreement. I will approach the EC this fall concerning which committee should champion the soot blower controls, failures, etc.

Question: can FD fan trips be staggered to save the ID fans during high furnace pressure trips? Does SFAF and SFBL want to tackle looking at recommending staggering FD fan trips on high furnace pressure trips to save the ID fan?

- Single fan / multiple fans / Steam driven ID fans, tuning

- 2oo3 voting? Look at filtering? MFT at +2, all fans at +4, Stagger trips? Go hard negative when all fuels tripped.

Afternoon session # Members 9 / # Visitors 8 visitors

- C.A. Vossberg reviewed presentation to SFBL regarding refractometer adjustments to off-line tests during start-up conditions.  Committee will be looking for a response from SFBL.

- Reviewed discussions from morning session and how to proceed with action items.

New Business: SSO methods and requirements jcb 092126

- Jumper and Bypass systems: Should more guidance on this be in BLRBAC documentation?  Numerous different terms are currently used in BLRBAC documents.  JC Browning will propose changes for the next meeting.

- Discussion about IT/OT separation.  Cameras can be in either category depending on their function and use.

- Discussion about Robot spout cleaner.  No guidance from BLRBAC is currently in place.

- Dissolving tanks: level, Baume, density, TA, TTA?  Discussion about these measurements and best practices.

- Question about rapid drain valves failing and which vendor for the actual “valve” is most successful.

  - Dissolving tanks: Level, Baume, density, TA, TTA? Discussed the various means of DT density control. Why is DT temperature not a Class 1 item. Provides good correlation, meaningful high and low temp alarm. Question about measuring Baume and the “pots” needed to take a sample.

2:00pm, meeting adjourned

The revised Instrumentation and Controls Guidelines and Check list has been posted for review on the BLRBAC website for at least the minimum of 60 days as required by the BLRBAC operating procedures and bylaws.  We will now put the revised guidelines to a vote.  Could all voting regular member representatives please stand?  All in favor of approving the revised Instrumentation guidelines. Any opposed?  Let it be noted that the revised Instrumentation guidelines have been approved.

7.5	MATERIAL & WELDING – Laura Nicol

MATERIALS & WELDING Subcommittee Meeting REPORT

The Materials and Welding (M&W) Subcommittee met in Open Session on Monday morning, October 5, 2026.

The meeting was opened at 8:00 am with a review of the BLRBAC Anti-Trust Statement.

# Attendance

Six (6) members and four (4) voting alternates out of twelve (12) attended. Three (3) additional alternates also attended. There were thirty-six (36) guests. 49 total in attendance

- Kindly request rectangle tables for April 2027 meeting

- Several members have now missed multiple meetings

  - National Boiler Services

  - Georgia Pacific

# Discussion

- Opened meeting with a Review of the BLRBAC Anti-Trust Statement.

- Introduction of attendees

- Had quorum and minutes from April 2026 were reviewed and approved.

- Reviewed the updated material and welding document – unanimously approved

  - Action: The SG requests Executive Committee to approve the updated document.

- Presentation #1 – Legacy – Billy Collett – presented the weld build up information that has been included into the Material and Welding Subcommittee

  - MIG – downhill, 0.035” is the best for weld build up – for big areas of WOL

    - Welder must be tested on downhill orientation

    - Short circuit arc deposit method to limit temperature

    - Dan Krekeler: How fast do you go with MIG?

      - Steve Harville: The puddle will tell you

      - Bill Burns: 18” per minute for automatic welding is a typical deposition rate

    - Dan Krekeler: What is the recommended NDE?

      - Billy Collett: MT or PT. X-ray is difficult to do the rough nature of WOL

  - Make sure the welders know it is okay if there is burn through

    - Make sure to share the information; the wall may be too thin to weld correctly

  - TIG okay for small areas

    - Do one layer, let it cool, do a second layer

    - Don’t rush it.

    - Wrap the toes of the weld

  - Small area = couple inches x couple inches

  - Large area = 12” x 12”

  - Welding with water in the tube is challenging

    - Changes the heat absorption profile

    - There noise because the water is boiling

- Dan Krekeler: Where you touch it and where you pull out is the area of concern for WOL

  - Legacy recommends “wrapping”

- Sugaring on the ID, how does it affect the tube?

  - Billy Collett: It is an oxidization

  - Cathrine Noble: Surface is more prone to damage

  - Laura Nicol: More of a long-term issue. It is a sign of the temperature the tube has seen, cause sanitization (Chrome migrating to the carbon)

- Bobby Johnston (Johnston Construction): what if there is a wire wheel cut that has been repaired?

  - Recommend X-raying the repair weld

  - Dan Krekeler: willing to keep it if the tube is good repair and similar to a regular weld (circumferential not longitudinal)

- Bill Burns: Remember SAC is different beast

- Presentation #2 – Legacy – Steve Harville – WOL without peel-back

  - 37.5 degree peel back is typical and what was tested, easier to weld

    - 30 degree – harder to tie into the clad

  - GP has been using the no peel back for 6 years

    - Most customers have been going to the no-peel back method

  - Dan Krekeler: will there be an issue long term?

    - Steve and Billy: no known issues

  - Cathrine Noble: Have you done tensile testing?

    - No

  - Dan Krekeler: how do the OEM do it?

    - In the shop – Andritz peels back

    - In the shop – B&W peels back

  - Dan Krekeler: can see issues when the carbon is pulled into the cap

    - Cap pass will disappear if there is significant dilution

  - Laura Nicol: Do you have a specific non-peel back weld procedure?

    - No

  - Recommend using 383 filler metal for cap filler metal

- Presentation #3 – Global Cellulose Fibers (GCF) Corporation – Dan Krekeler – Repair vs. Replace

  - Provided helpful tips on when a repair transitions into a replacement.

Lunch Break at 11:25 am

- Presentation #4 – Acuren Inspection – Cathrine Noble – Neutral Axis Cracking in Boiler Tubes

  - ID initiated, where the extrados (tension) and intrados (compression) meet

    - due to fatigue related

  - Action: Review in Spring 2027 to determine section and scope of neutral axis cracking

- Presentation #5 – Acuren Inspection – Cathrine Noble – Clearwater Paper Econ Tube Cracking

  - From the mill

  - Lab uses OES

  - Field uses PMI – but does not distinguish between carbon steels

    - Carbon is too small to be detected by standard PMI

  - LIBS – could tell you the carbon

- Reviewed Spring 2027 Topics

  - Solicited (victims) volunteers

- Presentation #6 – B&W – Laura Nicol – Drum Materials

  - Types of materials used in drums

  - How grain size affects toughness (aka – ductility or “transition temperature”

  - Carbon equivalency – to determine welding information

  - Evaluating existing drum

    - Life expectancy

    - Larson-Miller Parameter (LMP)

  - NBIC Repair Implications

    - PWHT and Repair Recommendations

    - Check with your Authorized Inspector and Jurisdiction

# Action Items for Future Meetings

- Follow up with Executive Committee on the updated Materials and Welding Document

  - Bill Burns to email contractors requesting help

- Presentations for Spring 2027:

  - Economizer Issue from Fall 2026 (IP – James Hendrix)

  - Master Hand Hole Caps or Blind Nipples (Andritz)

  - Inspection/Repair of composite interface transition line (Rudy Haraga)

  - Creep findings and inspection methods

  - 304L Historical Cracking Issues (Valmet)

  - Economizer Lower Header Failures

  - Weld Overlay vs Co-Extruded Tube Material

  - Boiler Alterations vs Repairs – NBIC

  - Generating Bank lessons learned/best practices (Legacy)

    - Swagging: ID Control

    - Check hydro locally with hand pump before main hydro (RMR past practice)

    - Hardness Recommendations

  - Essential verse Non-Essential – WPS/PQR

    - Welding Qualification Variables (Rayco)

Adjourned: 2:15 pm

7.6	PERSONNEL SAFETY – Steve Morrison

BLRBAC Personnel Safety Subcommittee Meeting Minutes – 10/5/26

Morning Session – Open attendance

- Called to order at 8am

- Read and displayed the anti-trust statement

- Introductions of attendees – Total of 39 attendees, 3 subcommittee members, 36 guests

- Covered the agenda for the open morning session

  - Incident investigation review

    - Woodland Pulp

    - Nippon DynaWave

  - Lundberg/Jansen Training Program

  - FORNAX Training Program

  - Valmet PPE

- Industry Incident Review

  - Showed the link to the Chemical Safety Board (CSB) website and how to navigate to the incidents

  - Discussed the sequence of events for Woodland Pulp

  - Discussed the sequence of events for Nippon DynaWave

- Asked for feedback on proposing personal H2S monitors as an addition to the Guideline

  - Current verbiage: If the recovery boiler building houses any systems that contain acids (i.e., demineralizers) or low pH solutions, these should have a separate sewer, storage,

and drainage system to prevent the formation of hydrogen sulfide (H2S) gas when

liquor containing wastes mix with acids. Acid and caustic storage should be

separately diked according to OSHA Standards. Areas where hydrogen sulfide

may be present should be equipped with continuous monitors and alarms.

    - H2S personal monitoring include as a BLRBAC requirement in addition to the continuous monitors – thoughts

    - Surveyed the members and audience on current mill practices

- Lundberg/Jansen training program presentation

Break 8:55am – 9:10am

Open Personnel Safety Continued 9:10am – 10:30am

- FORNAX training program presentation

- Showed audience how to access BLRBAC Guidelines, specifically the Personnel Safety and Training Guideline

- Showed audience how to access Chemical Safety Board website

- WL Gore Vulcan PPE presentation

- Circulated product samples around the audience

Adjourned the meeting at 10:55am for lunch

Afternoon Session:

- Called to order at 1pm

- Present members: Sam Dean (Rayonier Adv Mat), Steve Morrison (GP), Wayne Yenne (Fornax) – Do not have a quorum.

- Not present members: Brook Holland (Rayco), Justin Helton (Andritz), Tom Edwards (Diamond Power), Mathew Glann (Irving), Grey Gurkin (IP), Zack Payne (Andritz), Fransico Britt (FM), Jake Dowland (GP)

- Membership Changes: Greg Sallee (B&W) added to the subcommittee.

- H2S protection review within the current Guideline:

  - Ask for feedback for members on including personal H2S monitors within the Guideline

  - Should it be best practice or blanket statement similar to continuous monitoring language in the Guideline

  - Consensus was for the personal H2S monitoring to be a requirement vs. best practice

- Guideline review

  - Add the Personnel Guideline document on the BLRBAC website for review

  - Next meeting agenda - open session for review of the proposed changes of the Guideline in the morning and then actually do the edits (to a DRAFT document) in closed afternoon session with the intent of updating the entire Guideline before submitting to executive committee for approval – Estimate Fall 2027

  - Review chapter 1 and 2 for Spring – Review offline (focus on the editing process)

  - Section 1 review:

    - Sam Dean

    - Wayne Yenne

  - Section 2 review:

    - Greg Sallee

    - Steve Morrison

- Close session at 2pm

7.7    PUBLICITY & NEWS – Nick Quigley

No new update.

7.8	 SAFE FIRING OF BLACK LIQUOR – Sarah Henke

BLRBAC SFBL FALL MEETING DRAFT MINUTES - Fall 2026

Monday  October 5th -  8:30  am – 4 pm

8:30 am	--Noon Safe Firing of Black Liquor Subcommittee – (CLOSED meeting members only)

1 pm to 4 pm	Safe Firing of Black Liquor Subcommittee - (OPEN)

# Proposed Agenda:

- Open the meetings.  Both Closed and Open.

- Reviewed BLRBAC Anti-Trust statement. Both closed and open meeting.

- Introduce members and guests. 16 in closed (1 alternate) and 50 members/ guests in open.

- Review and approve the April 2026 minutes.

- New Business: Review any open items brought up to the subcommittee before the Fall 2025 Meeting.

- Review the EC feedback from the large tube leak logic revisions

- Going with large tube leak logic (not sudden large tube leak or large leak) verbiage

- Will change wording in Appendix B checklist to "Provided all required checks are satisfactory; it is permissible to reopen the feedwater valve and restart the boiler."

- Need better background on why subcommittee wants high furnace or low drum level trip, mainly for large external leaks

- Section 15.8 Sudden, large tube leak logic is a confusing paragraph. Section to be completely re-written

- Sarah to get more guidance from EC and will revert in Spring.

- Review the suggested changes from the instrumentation subcommittee – C.A to join at 1030-11am

- Review the suggested changes from the auxiliary fuel subcommittee

- How to prove burner is on? Manual valves can be shut and burner might not be on but showing on. “Ping-ponging” between subcommittees. Gas pressure and flow

- Note the above/below 70% solids for min 58 or 62 comes from the testing frequency

- How do people prove liquor is out of furnace? “All black liquor gun gates proven closed?” Change to figure 1 to add that verbiage. If pump down there could still be some gravity fed black liquor.

- Comment from Rudy on how to we handle earthquakes and ESPs.

  - How should mills react? ESP or MFT not a bad idea. Safe to drain the boiler

- Old Business:

- Isolating waste streams- there is nothing in the document that diagrams isolating waste streams during a purge in the liquor. Direct injection of waste streams into the liquor. Prove valve shut? Update from Peter in the fall to mark up changes. Cross reference waste streams.

  - Figure 2 add a block to prove all black liquor header direct injected waste steams isolated.

All other items to be discussed in Spring.

  - Agitator amp alarm procedure- Review Jason’s comments

- Immediate attention needed if you are running on back up (emergency) agitation with loss of a primary agitator. Ryan Henry of GBP to present progress. – Delayed

- DT FUNCTIONAL TESTING – What do we need to do here? Create a sample DT functional checklist. Someone to volunteer theirs. Will be added to appendix.

- SFBL need to address explosion technology for cleaning boilers? How do we address? How much force on the tubes? And how much is safe? Are there any operating boilers in NA with this? If not, maybe table the question.

- CONTINUE DISCUSSION FOR HIGH SOLIDS FIRING WITH SARAH INPUT.  Sarah/Ryan to have new findings.

- Jay Dilworth to present on using air to cool the DT agitator shaft other than water. – Jay is not attending so this will be delayed.

- Open item discussion and questions.

Question around how often ops do black liquor solids testing.

Question around rapid drain valves.

- DT incidents to review if any submitted

  - One submitted to review

  - Classified as an explosion

- Explosion videos if any submitted - none

- Close meetings as needed (closed and open).

7.9     WASTE STREAMS - Paul Seefeld - Chairman

Did not meet in the Fall of 2026

The revised Waste streams Guidelines have been posted for review on the BLRBAC website for at least the minimum of 60 days as required by the BLRBAC operating procedures and bylaws.  We will now put the revised guidelines to a vote.  Could all voting regular member representatives please stand?  All in favor of approving the revised Waste streams guidelines. Any opposed?  Let it be noted that the revised Waste Streams guidelines have been approved.

7.10	WATER TREATMENT – Tom Przybylski/PSA - Chairman

BLRBAC Fall 2026 Water Treatment Subcommittee meeting minutes

- The water treatment subcommittee met in open session for morning and afternoon sessions with 8 of 15 subcommittee members in attendance.  There were 6 guests.  The afternoon session had 9 of 16 subcommittee members and 7 guests.

- The session started with a review of the BLRBAC antitrust statement.

- We did not start with a quorum, so the morning started with tentative wording of the deionization project.

- There was discussion about the vessel integrity testing, who has authority, how often testing should occur, and how well it aligns with the already-approved condensate section.  Deionization vessels were only recommended for testing as dictated by the local authority having jurisdiction.  Liners were recommended for spark testing when resin was removed for replacement.  This coincides with a 5-year interval based on the typical life of cross-linked resin.  We aligned the vessel integrity testing in the condensate section (polishers) with the ones in this document (this will be submitted for approval once the deionization document is ready for review).

- Meeting minutes from last fall were approved once a 7th subcommittee member arrived to make a quorum.

- Upon arriving at a quorum, we approved the addition of Daniel Lishbrook from PSA to the subcommittee.  We reviewed the attendance roster and sent inquiries to some members who were not in attendance.  Peter Fogg (GP) has requested to be removed from the subcommittee. Oscar Guevara from Valmet requested to join the subcommittee.  We noted his request and will vote in the spring session, since he was unable to attend the afternoon session this afternoon, potentially affecting a quorum.

- The quorum also afforded us the opportunity to review the minutes from 2026.  The minutes were approved as written.

- A discussion about valve inspection and valve integrity was a major point of discussion.  While rubber-lined pinch valves are known failure points, it is not feasible to remove them for inspection.  Keeping in mind which valves are critical for demineralized water quality, we opted to require double block and bleed valves for regenerant into a deionization vessel.  Service outlet valves are also required to have manual block valve, with a bleed valve in the middle as recommended.

- The afternoon session started with discussion about water quality testing.  Specifically, Tappi has documentation that does not align with what we had, and is much more in depth that our guidelines.  Operating companies in attendance noted that their corporate guidelines are not as stringent as Tappi.  We elected not to reference Tappi, and recommended minimum testing that of 1x/shift, with testing more frequently to be considered if there is no continuous on-line instrument that is also.

- Linda Trinh from Sylvamo requested joining the subcommittee.  This was voted on and approved.

- We finished the meeting with a review of SOPs including off-spec water, instrumentation verification, including the nuances of testing pH of high-purity water.

- The meeting adjourned at 3:25PM

## Non BLRBAC organizations:

## 8.0   AMERICAN FOREST & PAPER ASOCIATION RECOVERY BOILER

## REPORT: See Appendix III – Slide Presentation) – Wayne Grilliot

The American Forest & Paper Association (AF&PA) Recovery Boiler Program was established in 1974 to help identify the root cause of recovery boiler critical incidents and explosions.  The AF&PA Recovery Boiler Program assists companies in improving the safety, integrity, and reliability of recovery boiler operations.  Recovery Boiler Program membership is open to all companies that operate recovery boilers.  Program activities are funded by member company dues.

The Recovery Boiler Program is under the direction of a Steering Committee which includes Stephen Cox (International Paper), Jeff Wagoner (International Paper), Greg Burns (Domtar), Alarick Tavares (Smurfit Westrock) and Wes Hill (Georgia-Pacific).  The Steering Committee sets Program priorities based on Member Company Input, BLRBAC Incidents, and Industry Needs.

The Recovery Boiler Program provides a forum for companies to develop information to help evaluate Safe Operating Procedures, Organization and Training, Maintenance Programs, Specifications and Construction, and Research & Development Programs.  Documents developed by the Program include Reference Manuals, Audit Guidelines, Best Practices, Training Aids, Checklists, Textbooks, and Studies.  The Program sponsors R&D projects for Safety Improvements and Process Improvements.  This helps drive improvements in Safety, Operations, Maintenance, and Recovery Boiler Integrity.

Available documents on the AF&PA Recovery Boiler Website include Publications, Studies, Training Aids, Standards, and General Program Information.

AF&PA Recovery Boiler Program Website:

http://www.afandpa.org/our-industry/recovery-boiler-program

9.0    TAPPI ENERGY, RECOVERY, RECAUST (ERR) Committee REPORT

– ERR Committee Daniel Franco

10.0   WESTERN CANADA BLRBAC REPORT – Jason Shaw for Angelo Porchetta

## Western Canada BLRBAC – Spring 2026 Meeting Summary

11.0   ACTIVITIES OUTSIDE NORTH AMERICA REPORTS:

There were no reports from organizations outside of North America.

12.0   OPERATING PROBLEMS SESSION REPORT – David Tjaarda

Operating Problems Session Report Out

The session began at 1:00 PM on 10/6/26, and was facilitated by David Tjaarda of Smurfit Westrock the Vice chair of the Executive Committee with assistance from Laura Nicol of B&W and Andy Jones of SHB.

There were 18 questions submitted in writing.  Additionally, one overseas boiler explosion event was reviewed with pictures by Rudy Haraga of Fornax Services.  Two other video clips were shared and discussed.  We were able to talk through all but one question.

Questions topics

were related to:

- Utilization of AI to improve boiler safety

- Meeting SO2 emissions

- Managing sulfidity and having good targets

- Adding sulfur make up to the process

- Limiting TRS

- Utilization of Nalco TRASAR

- Recovery furnace excess oxygen control

- Spout design

- Controlling reduction efficiency

- Managing corrosion at the composite to carbon transition line

- Cleaning the air side of steam coil air heaters

- Large tube leak logic

- Operator training on day off

- Furnace pressure trip point settings

- Preventing smelt leak from insertable spouts

The session concluded at 2:25 PM.

13.0 CLOSING COMMENTS:

CHAIRMAN: Gregory Burns

BLRBAC would like to recognize a BLRBAC icon who has served BLRBAC over the years in several leadership roles.  He has led the ESP subcommittee and was a previous Chairperson of the BLRBAC Executive Committee, He was never shy about sharing his opinion and always made the Operating Problem session interesting with stories that were always on point.  Scott Moyer presented Frank Navojosky with his award for years of service to BLRBAC.

CHAIRMAN: Gregory Burns

That concludes our Main Committee Meeting this morning.  Thank you all for your attendance and your time away from home and work.  Our next meeting will be April 5th, 6th and 7th 2027, the next Fall meeting will be October 4th, 5th and 6th 2027 and both meetings will be here at the Atlanta Airport Hilton Hotel.  The Executive Committee strongly encourages you to register and stay at the Hilton.  Be on the lookout for that registration email in late January.  Please spread the word to increase participation in these meetings.  We really need more participation from the mills and mill representatives taking on some leadership roles in the subcommittees.

With that I'll will now entertain a motion to close the Main Committee meeting.   Second?    The Main committee Meeting is now closed.  We will have our Technical Presentation starting in about 15 minutes.

Thank you all and have a Safe trip home!

APPENDIX I

Incident Reports

APPENDIX II

2026 Fall Meeting ESP Subcommittee Report

Frank Navojosky

APPENDIX III

AF&PA Report

Wayne Grilliot

mmittee Vi

APPENDIX IV

Presentations

On-Site Recovery Boiler ESP Training and DCS Readiness Assessment – Rudy Haraga – Fornax Services

Reliable Dissolving Tank Density Measurement - C.A. Vossberg – Electron Machine

Future-Proofing Existing Flue Gas Systems - Jonas Gestranius - Valmet